|  | Bedford Materials Co., Inc. 7676 Allegheny Rd Manns Choice, PA 15550 Phone: (814) 623-9014 Fax: (814) 623-9199 E-Mail: bedmat@bedford.net |
| --- | --- |

5M74
B-STAGED (SEMI-CURED)
CLASS 180(C POLYESTER RESIN
ON HIGH STRENGTH GLASS CLOTH

5M74 IS HIGH-STRENGTH WOVEN GLASS CLOTH IMPREGNATED WITH A HIGH TEMPERATURE POLYESTER RESIN.  IT HAS A TACKY FINISH AND IS SUPPLIED WITH A POLYETHYLENE SEPARATOR SHEET.  SUITABLE FOR 180(C APPLICATIONS.

TYPICAL PROPERTIES (UNCURED)

THICKNESS, BASE CLOTH                              0.007”
RESIN CONTENT                                               45 – 50%
TENSILE STRENGTH                                        200-220 LBS./IN. WIDTH

RECOMMENDED CURE                              4 HRS @ 150(C

SHELF LIFE                                                     6 MONTHS WHEN STORED BELOW 70(F

TEMPERATURE RATING (CURED)            CONTINUOUS SERVICE AT 180(C

APPLICATIONS                                              COIL BANDING AND WRAPPING

The information contained herein is intended as a guide and should not be construed as a performance guarantee as the company has no control over the manner in which others may employ the product.