|  | Bedford Materials Co., Inc. 7676 Allegheny Rd Manns Choice, PA 15550 Phone: (814) 623-9014 Fax: (814) 623-9199 E-Mail: bedmat@bedford.net |
| --- | --- |

Technical Data 96-580

8929
Silicone Resin Coated Glass Cloth
For 200°C Applications

| ## Application Bedford Materials 8929 silicone-resin-coated glass cloth and tapes involve the use of a straight weave, continuous filament fabric, treated with a fully cured silicone resin. This flexible Class H insulation offers good dielectric strength at high temperatures, great cut-through, chemical and tracking resistances and hence great overload protection. These products are generally used as flexible layer, wrapper and tape insulation in high temperature applications. ## Advantages Dielectric strength is retained at elevated temperatures. Meet the requirements of NEMA, ASTM and MIL-17205C, where applicable. Meet the performance requirements for Class H thermal service. | Specifications (Typical Values) 8929-1 8929-2 8929-3 8929-4 _ Thickness, Treated (Inches)……….. 0.0035 0.004 0.005 0.007 0.010 0.010 0.013 Thickness, Base Fabric (inches)…… 0.002 0.002 0.002 0.003 0.004 0.007 0.007 Weight, Approximate (lbs./sq. yd.)… 0.22 0.26 0.32 0.43 0.65 0.80 0.96 Tensile Strength (lbs./in. of width) MD………………………………. 70 70 70 100 100 300 300 CMD…………………………….. 40 40 40 70 70 240 240 Dielectric Strength, Minimum Average, ¼ in. Dia. Electrodes, Short Time Method (volts/mil) as Received……………………. 1,500 1,500 1,500 1,400 1,300 450 650 as Received, Bent…………….. 1,060 1,250 1,240 1,145 1,050 400 465 168/250, Bent…………………. 900 1,065 1,055 975 900 370 400 96/23/0………………………… --- 1,400 1,200 1,300 1,200 --- --- 96/23/96………………………. --- 1,000 600 900 800 --- --- Ordering Information Standard tape widths are available on 1 inch ID cores in rolls 36 and 72 yards long. Also available approximately 36 inches wide in standard 36, 50 and 100 yard rolls and in master rolls approximately 350-400 yards long. Specify quantity, length and width and thickness required. Bedford Materials has no control over the final application of the product by others, therefore, the information contained herein is intended as a general guide to product use and should not be construde as a warranty. |
| --- | --- |