|  | Bedford Materials Co., Inc. 7676 Allegheny Rd Manns Choice, PA 15550 Phone: (814) 623-9014 Fax: (814) 623-9199 E-Mail: bedmat@bedford.net |
| --- | --- |

Inorganic Paper Composites

| CeQUIN4 I Paper Composites CeQuin I composites have replaced asbestos containing composites as high temperature, low cost insulation materials. CeQUIN I papers are manufactured by Quin-T Corporation and offer a realistic replacement for asbestos papers (Quinorgo and Quinterra). CeQUIN I papers are a family of inorganic fibers bonded together with organic binders. Most of the papers are recognized in UL systems. Composites of CeQUIN I and glass cloth and polyester film are recognized in systems up to 220(C. | CeQUIN I/Paper/Glass Cloth |
| --- | --- |
|  | CeQUIN I | Glass | CeQuin I | Tks. (In.) | Yield | Dielectric Strength Volts | Tensile Strength Lbs./In. Width MD CMD | Tear Strength Graves Lbs. MD CMD |
|  |  |  |  |  | Lbs./Sq. Yd. | Sq. Yds/Lb. |  |  |  |
|  | .005 | .004 | - - - | .009 | .42 | 2.38 | 1,250 | 125 | 100 | 12 | 9 |
|  | .007 | .004 | - - - | .011 | .52 | 1.92 | 1,650 | 125 | 100 | 12 | 9 |
|  | .010 | .004 | - - - | .014 | .66 | 1.52 | 3,150 | 125 | 100 | 13 | 9 |
|  | .005 | .004 | .005 | .014 | .70 | 1.43 | 2,600 | 185 | 147 | 14 | 12 |
|  | .007 | .004 | .007 | .018 | .90 | 1.11 | 3,800 | 198 | 158 | 14 | 15 |
|  | .010 | .004 | .010 | .024 | 1.21 | .83 | 5,100 | 218 | 158 | 19 | 14 |
|  | Glass | CeQUIN I | Glass |  |  |  |  |  |  |  |  |
|  | .004 | .005 | .004 | .013 | .61 | 1.64 | 1,500 | 170 | 170 | 14 | 14 |
|  | .004 | .010 | .004 | .018 | .86 | 1.16 | 2,300 | 218 | 215 | 19 | 17 |
|  | .004 | .015 | .004 | .023 | 1.03 | .97 | 3,850 | 210 | 210 | 23 | 17 |
|  | NOTE: Other constructions available on request. CeQUIN I/Paper/Polyester Film |
|  | CeQUIN I | Film | CeQUIN I | Tks. (In.) | Yield | Dielectric Strength Volts | Tensile Strength Lbs./In. Width MD CMD | Tear Strength Graves (Lbs.) MD CMD |
|  |  |  |  |  | Lbs./ Sq. Yd. | Sq./ Yds. Lb. |  |  |  |
|  | .003 | .001 | - - - | .004 | .19 | 5.26 | 4,800 | 22 | 25 | 3 | 3 |
|  | .005 | .001 | - - - | .006 | .31 | 3.23 | 5,800 | 23 | 25 | 3 | 3 |
|  | .005 | .0015 | - - - | .0065 | .35 | 2.86 | 7,200 | 33 | 35 | 5 | 4 |
|  | .005 | .005 | - - - | .010 | .58 | 1.72 | 12,200 | 76 | 77 | 12 | 15 |
|  | .010 | .001 | - - - | .011 | .57 | 1.75 | 6,400 | 32 | 22 | 5 | 4 |
|  | .010 | .003 | - - - | .013 | .72 | 1.39 | 10,000 | 60 | 73 | 11 | 11 |
|  | .007 | .005 | - - - | .012 | .69 | 1.45 | 14,000 | 100 | 120 | 14 | 15 |
|  | .003 | .001 | .003 | .007 | .33 | 3.03 | 5,300 | 30 | 28 | 4 | 4 |
|  | .005 | .002 | .005 | .012 | .67 | 1.50 | 8,200 | 46 | 54 | 9 | 8 |
|  | .007 | .0015 | .007 | .0155 | .82 | 1.22 | 8,000 | 52 | 53 | 9 | 7 |
|  | Film CeQUIN I Film |  |  |  |  |  |  |  |
|  | .001 | .005 | .001 | .007 | .38 | 2.63 | 9,500 | 41 | 41 | 6 | 6 |
|  | .002 | .005 | .002 | .009 | .55 | 1.82 | 12,000 | 80 | 100 | 13 | 13 |
|  | .001 | .010 | .001 | .012 | .66 | 1.52 | 9,500 | 53 | 57 | 10 | 8 |
|  | NOTE: Other constructions available on request. |

Bedford Materials has no control over the final
applications of the product by others, therefore,
the information contained herein is intended as
a general guide to product use and should not
be construed as a warranty.

4 Quin-T registered TM for its ceramic mineral paper