|  | Bedford Materials Co., Inc. 7676 Allegheny Rd Manns Choice, PA 15550 Phone: (814) 623-9014 Fax: (814) 623-9199 E-Mail: bedmat@bedford.net |
| --- | --- |

Technical Data 96-580

NEMA – 5JF04 Tan
Varnished Glass Cloth Extremely Flexible Class 180C

Life Rating – 50,000 hrs. at 180ºC

| ## Application for 5JF04 Bedford Materials 5JF04 Class consists of NEMA straight weave continuous filament glass fabric coated to specified thickness with a flexible insulating varnish. Meets requirements of MIL-I-17205, grade O. ## Advantages Excellent for taping, layer, wrapper and phase insulation in electrical equipment wherever flexibility, and high dielectric strength are required. Used on original equipment and repair for armature and stator coils, transformers and other applications where a flexible and high temperature electrical barrier is needed. | Specifications (Typical Values) Color………………………………………….. .. ---------- ---Tan------------- Finished Thickness (inches)………..…………… 0.007 0.010 0.012 0.015 Thickness, Glass Fabric Base (inches)…….…… 0.003 0.007 0.007 0.007 Weight, Approximate (lbs./sq. yd.)…………….. 0.41 0.69 0.84 1.02 Tensile Strength, Warp (lbs./in. of width) WARP 100 300 300 300 FILL 70 200 200 200 Gurley Stiffness (MG) MD 180 500 500 500 CMD 120 400 400 400 Dielectric Strength (V/M) C-96/23/0…………… 1,600 1,300 1,250 1,200 (V/M) C-96/23/96…………………. 900 500 500 500 (V/M)(Bent) C-168/23/50………… 1,500 1,000 1,000 1,000 (V/M)(Bent) E-168/130………….. 1,800 700 700 700 (V/M)(Bent) E-168/180………….. 1,000 400 N/A N/A Power Factor (60 cycle) C-96/23/0…………….. 0.05 0.05 0.05 0.05 C-96/23/96……………. 0.20 0.20 0.20 0.20 Dielectric Constant (60 cycle) C-96/23/0………. 5.0 5.0 5.0 5.0 C-96/23/96…….. 8.0 8.0 8.0 8.0 Toluol Resistance (immersion)…………………. No Effect After 3 Minutes Ordering Information Supplied in 36 yard long rolls approximately 36 inches wide on 1 ½ inch ID cores and in master rolls approximately 350-400 yards long. Also supplied in tape slit to width as specified. Other thicknesses available on negotiation. |
| --- | --- |

|  | Bedford Materials Co., Inc. 7676 Allegheny Rd Manns Choice, PA 15550 Phone: (814) 623-9014 Fax: (814) 623-9199 E-Mail: bedmat@bedford.net |
| --- | --- |

Technical Data 96-580

NEMA – 5JF44 Tan
Varnished Glass Cloth Extremely Flexible Class 180C

Life Rating – 50,000 hrs. at 180ºC

| ## Application for 5JF44 Bedford Materials 5JF44 Class is a straight weave .004 inch thick (L.C.) continuous filament glass fabric coated to specified thickness with a flexible insulating varnish. Meets requirements of MIL-117205, grade O. ## Advantages Excellent for miscellaneous electrical insulation application where flexibility and good thermal aging properties are desired. An economical flexible insulation for taping layer, wrapper, and phase applications. | Specifications (Typical Values) Color………………………………………….. .. ---------- ---Tan------------- Finished Thickness (inches)………..…………… 0.007 0.010 0.012 0.015 Thickness, Glass Fabric Base (inches)…….…… 0.004 0.004 0.004 0.004 Weight, Approximate (lbs./sq. yd.)…………….. 0.44 0.65 0.76 0.86 Tensile Strength, Warp (lbs./in. of width) WARP 150 150 150 150 FILL 120 120 120 120 Gurley Stiffness (MG) MD 170 220 400 425 CMD 85 150 375 350 Dielectric Strength (V/M) C-96/23/0…………… 1,400 1,300 1,300 1,300 (V/M) C-96/23/96………….……. 800 800 800 800 (V/M)(Bent) C-168/23/50……….. 1,300 1,200 1,200 1,200 (V/M)(Bent) E-168/130………….. 1,600 1,500 1,500 1,500 (V/M)(Bent) E-168/180………….. 900 800 N/A N/A Power Factor (60 cycle) C-96/23/0…………….. 0.05 0.05 0.05 0.05 C-96/23/96……………. 0.20 0.20 0.20 0.20 Dielectric Constant (60 Hertz) C-96/23/0………. 5.0 5.0 5.0 5.0 C-96/23/96…….. 8.0 8.0 8.0 8.0 Toluol Resistance (immersion)…………………. No Effect After 3 Minutes Ordering Information Supplied in 36 yard long rolls approximately 36 inches wide on 1 ½ inch ID cores and in master rolls approximately 350-400 yards long. Also supplied in tape slit to width as specified. Other thicknesses available on negotiation. Bedford Materials has no control over the final application of the product by others, therefore, the information contained herein in intended as a general guide to product use and should not be constructed as a warranty. |
| --- | --- |