|  | Bedford Materials Co., Inc. 7676 Allegheny Rd Manns Choice, PA 15550 Phone: (814) 623-9014 Fax: (814) 623-9199 E-Mail: bedmat@bedford.net |
| --- | --- |

Technical Data 96-580

5JF47 Tan (Low Cost)
Varnished Glass Cloth Class 180C

For 180ºC Applications

| Application for 5JF47 Bedford Materials 5JF47 is a straight weave .007 inch thick continuous filament glass fabric coated to specified thickness with a flexible insulating varnish. Meets requirements of MIL-I-17205, grade O. Advantages Excellent for miscellaneous electrical insulation applications where flexibility and good thermal aging properties are desired. An economical flexible insulation for taping, layer, wrapper, and phase applications. | Specifications (Typical Values) Color………………………………………….. .. (-------Tan------( Finished Thickness (inches)…..………………… 0.010 0.015 Thickness, Glass Fabric Base (inches)…….…… 0.007 0.007 Weight, Approximate (lbs./sq. yd.)…………….. 0.75 1.00 Tensile Strength, Warp (lbs./in. of width) WARP 220 220 FILL 170 170 Gurley Stiffness (MG) MD 500 500 CMD 400 400 Dielectric Strength (V/M) C-96/23/0…………… 1,200 1,200 (V/M) C-96/23/96………………… 500 500 (V/M)(Bent) C-168/23/50………… 1,000 1,000 (V/M)(Bent) E-168/130………….. 700 700 (V/M)(Bent) E-168/180………….. 400 N/A Power Factor (60 cycle) C-96/23/0…………….. 0.05 0.05 C-96/23/96……………. 0.20 0.20 Dielectric Constant (60 cycle) C-96/23/0………. 5.0 5.0 C-96/23/96…….. 8.0 8.0 Toluol Resistance (immersion)…………………. No Effect After 3 Minutes Ordering Information Supplied in 36 yard rolls approximately 36 inches wide on 1 ½ inch ID cores and in master rolls approximately 350-400 yards long. Also supplied in tape slit to width as specified. Other thicknesses available on negotiation. Bedford Materials has no control over the final applications of the product by others, therefore, the information contained herein is intended as a general guide to product use and should not be considered as a warranty. |
| --- | --- |